## Slide 1
Spontaneous parametric down-conversion
from nanostructured LiNbO3 resonators
2° Congresso Nazionale NQSTI
supra Nano-Optics milano Labs
February 6th, 2023

## Slide 2
Lithium niobate — a wonder material for (nano?)photonics
Bring these functionalities to the nanoscale!
Periodically-poled LiNbO3
Transparency from 350 nm to 5000 nm
Large electro-optic coefficient (r33 = −35 pm/V)
→ Pockels cells and Q-switching in the near-IR
Second-order nonlinearity (d33 = 27 pm/V)
  → Frequency up-conversion to the visible
Harmonic generation in Nd:YAG lasers
LiNbO3 Pockels cells

## Slide 3
Nanofabrication of lithium niobate
Andrea Toma
LiNbO3 is very hard and chemically stable
→ Challenging nanofabrication
Monte Carlo collision simulation
→
Ga+ focused ion beam machining
of LNOI thin films (500 nm)
+ High aspect ratio
+ Smallest spatial features
− Highly expensive
− Hardly scalable
→
→
→
Scanning electron microscopy
7˚
1 μm
Marzia Ferrera

## Slide 5
Back-focal plane imaging of the second-harmonic emission
LiNbO3
LiNbO3

## Slide 6
Visible second harmonic from a lithium niobate metasurface
L. Carletti1, A. Zilli2, F. Moia3, A. Toma3, M. Finazzi2,
C. De Angelis1, D. N. Neshev4, and M. Celebrano2
ACS Photonics 8, 731 (2021)
3
1
2
4
Resonance in the NIR at 820 nm
→ SHG in the VIS at 410 nm
Magnetic
dipole (MD)
resonance
50
0
|E|2 /|E0|2
Notes: Isabelle Staude, Tomas Santiago-Cruz
Ma LPR21: Pavg = 23 mW, 200 fs, 80 MHz, eta = 2.0e-6, gamma = 2e-6 / (0.033 W / 200e-15 / 80e6)

## Slide 7
An electro-optic integrated metasurface
Monolithic LiNbO3 architecture with Interdigitated electrode design
1 µm
Speed > 1GHz
Efficiency > 0.01/V
Notes: This slide can go

## Slide 8
SHG modulation with CW pumping
Agostino Di Francescantonio
Rachel Grange
A. Di Francescantonio1, A. Sabatti2, H. Weigand2, E. Bailly2, M.A. Vincenti3,
L. Carletti3, J. Kellner2, A. Zilli1, M. Finazzi1, M. Celebrano1, and Rachel Grange2
arXiv 2412.03422 (2024)
3
1
2
Notes: This slide can go

## Slide 9
Meta-optics with lithium niobate – Our perspective
A. Fedotova1, L. Carletti2, A. Zilli3, F. Setzpfandt1,
I. Staude1, A.Toma4, M. Finazzi3, C. De Angelis2,
T. Pertsch1, D. N. Neshev5, and M. Celebrano1
ACS Photonics 9, 3745 (2022)
1
2
3
4
5
NQSTI Spoke 6 − Topic A3: Integration of single-photon sources into lithium niobate

## Slide 10
A classical−quantum correspondence
Santiago-Cruz et al. Nano Lett. 21, 4423 (2021)
Experimental challenges
Low photon-pair yield from ultrathin platforms
Pairs are emitted over a broad angular range
→ Resonances to boost and control emission
→ Quantum−classical correspondence as a heuristic design tool
SPDC
ω
ω
2ω
d33
(s)
(i)
(p)
ω
ω
2ω
d33
SHG
Time reversal
Fedotova et al. Nano Lett. 20, 8608 (2020)

## Slide 11
Can we reduce the footprint to a single nanoresonator?

## Slide 12
λ = 1487 nm, Q = 13
Numerical design: eigenmodes of a LiNbO3 disc
M. Poloczek
λ = 1465 nm, Q = 37
λ = 1476 nm, Q = 11
Full vectorial simulations with Comsol+Matlab+Retop
No classical approach available to simulate SPDC
Eigenmode study of a disc (H = 500 nm, R = 1300 nm) in the telecom range

## Slide 13
Numerical design: eigenmodes of a LiNbO3 disc
M. Poloczek
λ = 1487 nm, Q = 13
λ = 1465 nm, Q = 37
λ = 1476 nm, Q = 11
Full vectorial simulations with Comsol+Matlab+Retop
No classical approach available to simulate SPDC
Eigenmode study of a disc (H = 500 nm, R = 1300 nm) in the telecom range

## Slide 14
Numerical design: boosting and beaming SPDC with resonances
Wang, Pan et al. Phys. Rev. Lett. 122, 113602 (2019)
Liu, Wang et al. Nat. Nanotechnol. 14, 586 (2019)
Electron microscopy
z
disc
groove
cut
1 μm
LiNbO3
SiO2
Cr
d
x
d
Directional emission
Inspired by Bragg gratings as SPDC beamers
Check with test dipole →
Resonance
size
Resonant enhancement
Purcell effect
Check with simulated SHG efficiency

## Slide 15
Measurements of photon pair emission
SHG raster imaging
z
5 μm
LiNbO3
SiO2
disc
groove
cut
g(2) =
Ncoi + Nacc
Nacc
M. Chekhova
V. Sultanov
Ncoi
Nacc
disc
CW pump
λ = 785 nm
P = 5 mW
t = 10 min
disc
cut
Notes: Us: 300 Hz/W DuongOME22: 15 Hz/W

## Slide 16
FIB milling
+ High aspect ratio
+ Smallest features
Biphoton rate order of magnitude better than previous reports from nanoparticles
Large luminescence from groove/cut
Implantation of FIB Ga+ ions?
EBL + dry etching
+ Larger areas
+ Less destructive
Andrea
Toma
Marzia
Ferrera

## Slide 17
The QuantumLiNbO team @ PoliMi
Michele Celebrano
Team member
Attilio Zilli
Project co-PI
Marco Finazzi
Project PI
Alfonso Nardi
Post-doc

## Slide 18
Acknowledgements
Attilio Zilli
Michael Poloczek
Yigong Luan
Michele Celebrano
Marco Finazzi
Simulations and SHG @PoliMi
Marzia Ferrera Andrea Toma
Nanofabrication @IIT (Genova)
Luca Carletti
Theory & calculations @ Uni. Brescia
Vitaliy Sultanov
Michael Poloczek
Emmanouil Kokkinakis
Tomàs Santiago-Cruz
Maria Chekhova
SPDC @Max-Planck (Erlangen)
Spesa finanziata a valere sulle risorse previste dal bando a cascata emanato da UNIMIB con DR 443/2024 prot. 53652 del 31/01/24, ai sensi dell’Avviso MUR n. 341 del 15 marzo 2022, nell'ambito del PNRR, M4C2 Investimento 1.3- Progetto NQSTI PE_00000023, finanziato dall'Unione europea- NextGenerationEU - CUP H43C22000870001 - Spoke 6 – bando a cascata prog. “NQSTI” – QuantumLiNbO.

## Slide 19
Summary and outlook
  LiNbO3 is emerging as a prime material for nonlinear nanophotonics
  Progress enabled by steady advances in nanofabrication capabilities
  Metasurface exhibit polarization-controlled second-harmonic steering
  Nanostructured resonator designed as a directional source of photon pairs
  → Directional emission still to be proven experimentally