## Slide 1
Novel phenomena in oxide
two-dimensional electron systems
Marco Salluzzo
Research Director CNR-SPIN
Napoli, Italy
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
Consiglio Nazionale delle Ricerche
Istituto SPIN - Napoli

## Slide 2
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
  EXPERIMENTAL
  Samples preparation
Yu Chen, M.Rath, CNR-SPIN
  Transport measurements on LAO/ETO/STO and LAO/STO
-Yu Chen,M. D’Antuono and D. Stornaiuolo UNINA and CNR-SPIN
-D. Preziosi CNRS-Strasbourg
  -B. Jouault CNRS-Montepellier
  Transport measurements and FE characterizations on LAO/ETO/Ca-STO
  J. Bréhin, M. Bibes, CNRS-Thales (Lab. A. Fert)
  XAS, XLD, XMCD, RIXS
  -Yu Chen, M. Rath, CNR-SPIN
  -C. Piamonteze, PSI-SLS
  -N.B. Brookes, G. Ghiringhelli, ESRF and Politecnico di Milano
  Structural HRTEM
  J. SantaMaria, M.Cabero Piris, UCM, GMFC Madrid
  THEORY
  Theory (DFT+U)
  -M. Verma and R. Pentcheva (LAO/ETO/STO), University of Duisbourg-Essen
  -J. Varignon (LAO/ETO/Ca-STO), CRISMAT, CNRS
  Theory (quantum transport, Model Hamiltonian)
  Yu Chen, A. Perroni, M. Trama, R. Citro

## Slide 3
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
Spin(orbi)tronics
Quantum(topological)
Electronics
Spin-orbit
coupling
2D-Ferroelectricity
2D-Superconductivity
2D-Ferromagnetism
Inversion and time reversal symmetry breaking in low dimensional systems give rise to novel physical phenomena and might allow the coexistence of order parameters which normally compete:
NOVEL PHYSICS AND NOVEL FUNCTIONALITIES
QUANTOX
ERA-NET EU H2020
GA No. 731473
IQARO Path-Finder
Horizon Europe
GA No. 101115190
PNRR MUR project
PE0000023-NQSTI

## Slide 4
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
STO-Based heterostructures: Novel Physical phenomena
(Nat. Mat. 278 (2016) )
High Tc-SC
LAO/ETO/STO
NdNiO2/STO
LaAlO3/STO
Ferromagnetic
and SC 2DEG
SC 2DEG
Multiferroic
2DEG
LAO/ETO/Ca-STO
Nature 572, 624 (2019)
Nature 427, 423 (2004)

## Slide 5
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
Ferromagnetism, Superconductivity, Ferroelectricity
S. S. Saxena et al. NATURE |VOL 406 | 10 AUGUST 587 (2000)
Heavy fermions
Tingyu Qu et al. https://doi.org/10.21203/rs.3.rs-2965127/v1
Co-intecalated NbSe2 (Co-NbSe2)
Rischau et al., Nature Physics 13, 643 (2017)
Talk by Inoue !
FE-STO
FM+FE+SC. in 2D?

## Slide 6
M. SALLUZZO (CNR-SPIN)
06/02//2025
q2DEG
FM (and SC) q2DEG
FE (and SC) q2DEG
FE and FM q2DEG
J. Bréhin, Y. Chen, M. D’Antuono, S. Varotto, D. Stornaiuolo, C. Piamonteze, J. Varignon, M. Salluzzo, and M. Bibes, Nat. Phys. 19, 823 (2023).
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
A metallic ferroelectric: the q2DEG based on FE Ca-STO

## Slide 7
∆n2D
(Pup-Pdown)
Remanent
Polarization
RsvsT
TC (FE)
Ferroelectric-like transition
M. SALLUZZO (CNR-SPIN)
06/02//2025
PLD growth of ETO and LAO on 1% and 2% Ca-STO
Anomalous Hall effect
Magneto-resistance hysteresis
Modular system for
Oxide
Deposition and
Analyses
Surface Analysis chamber,
AFM, STM, SPA-LEED, XPS, UPS
PLD chamber
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma

## Slide 8
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
Coupling between Ferroelectricity and magnetism in the transport
Electro-magnetoresistance emerging well-below Tc(FE)
J. Bréhin, et al. Nat. Phys. 19, 823 (2023).
VG (V)
RAHE (Ω)
MR (%)
Magnetoresistance
non volatile switching
Anomalous Hall resistance non volatile switching
Back-gate voltage
Is the 2DEG Ferroelectric and Ferromagnetic?
Are the two order parameters coupled?

## Slide 9
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
XMCD
XLD
3dxy
3dxz/3dyz
3dx2-y2
3dz2
2p1/2
2p3/2
L3
L2
x-rays
eg
t2g
FY: Bulk sensitive but interfacial sensitive to the Eu-magnetic moment
TEY: Interface Sensitive (probe depth 2 nm)

## Slide 10
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
XLD and XMCD in LAO/ETO/STO
3dxy lowest in energy as in LAO/STO
M. S. et al., Phys. Rev. Lett. 102, 166804 (2009)
M. S., et al. Adv. Mater. 25, 2333 (2013)
D. Stornaiuolo, et al. Nature Materials 15, 278 (2016)
50 meV
100 meV
Eu and Ti magnetic moment coupled: in-plane easy-axis, Tc =6-8 K

## Slide 11
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
TEY mode (interface sensitive) Ti L2,3 edge XLD across the FE transition
LAO/Ca(2%)-STO
LAO/ETO/Ca(2%)-STO
2 K BLACK T<TFE
40 K RED T>TFE
VG=0
VG=0
Clear effect of the FE-transition on the
TEY Ti-XLD spectra (probing the 2DEG Ti-states)
Signature of the FE-transition are seen in the Ti 3d-orbital splitting

## Slide 12
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
LAO/ETO/Ca(1%)-STO
TEY mode (interface sensitive) Ti L2,3 edge XLD SWITCHING
Strong XLD expected from off-centered Ti ions with respect to oxygen ions in the 2DEG: electric dipole
XLD depends on P direction: different electric dipole amplitude for different P states
Atomic multiplet simulations reproducing data indicate larger electric dipole in Pdn than Pup, consistent with DFT
Switchable dipoles in the 2DEG region: Ferroelectric-like switching
Pup ∆eg= -80 meV ∆t2g = -60 meV
Pdown ∆eg= -95 meV ∆t2g = -70 meV

## Slide 13
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
FY mode on Eu M4,5 edge XMCD is sensitive to the Eu-magnetization at the interface
-Effect of the remanent FE-polarization on the Eu-Magnetism (probing the 2DEG Eu 4f -states)
Magnetoelectric Coupling: change of 1.5% of the spin moment and of about 10% of the orbital moment at 0.5 Tesla
morb ∝-q
mspin ∝ -(5p-3q)
q
p
FY Eu-XMCD vs FE Polarization

## Slide 14
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
FY Eu-XMCD vs GATE VOLTAGE
Magnetoelectric Coupling: main modulation of the orbital moment of Eu2+
morb ∝-q
mspin ∝ -(5p-3q)
VG= -80 V
VG= +80 V

## Slide 15
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
SPIN-ORBIT QUBITS BASED ON OXIDE 2DEGs
Realization of a prototype of SO-qubit with oxide 2DEGs with fast control of spin quantum states through tunable spin-orbit coupling (TRL4). In particular we aim a reduction of of direct and indirect sources of decoherence with respect to state of art SO-qubits due to:
- intrinsic properties of oxide materials, in particular the reduced nuclear hyperfine interaction due to carriers characterized by 3d- orbital wavefunctions and small intrinsic inner nuclear field;
- large tunability of the Rashba SOC and of the giant STO dielectric screening, for the reduction of charge noise;
IQARO Path-Finder
Horizon Europe
GA No. 101115190

## Slide 16
M. SALLUZZO (CNR-SPIN)
06/02//2025
Secondo Congresso NQSTI, 05-07 febbraio 2025, Roma
A FE and FM 2DEG have been engineered using EuTiO3 delta-doping layer at the interface between LaAlO3 and FE Ca-SrTiO3
    - ferromagnetism demonstrated by XMCD
    -Anomalous Hall effect due to the interplay of magnetism and SOC
    -Non-volatile switching of the resistance, Hall-effect and magnetoresistance
    -XLD data show the the orbital splitting is modulated by the polarization switching and across the FE transition temperature
    - XMCD data show a modulation of the orbital magnetic moment of Eu-4f
    states by the electric field effect.
    -Spin-orbit qubits based on oxides
Summary